Single Wall Carbon Nanotubes Produced from Methane by Metal - Catalyzed

Sharif Hussein Sharif Zein1, Abdul Rahman Mohamed*1, P. Sesha Talpa Sai1 and

Noor Asmawati Mohd Zabidi2

1School of Chemical Engineering,

Engineering Campus, Universiti Sains Malaysia,

##### 14300 Nibong Tebal, S.P.S, Pulau Pinang, Malaysia

*E-mail: chrahman@eng.usm.my

2Chemical Engineering Program

Universiti Teknologi PETRONAS,

#### Bandar Seri Iskadaar

31750 Tronoh, Perak, Malaysia

The catalytic formation of carbon nanotubes has been frequently reported during decomposition of carbon monoxide and several hydrocarbons over supported iron, cobalt and nickel catalysts and extensive studies has been conducted regarding the growth of these filaments and its possible mechanism. Recently, carbon nanotube materials have been paid considerable attention due to their excellent properties and potential utilization. Most of the authors propose carbon nanotubes as a starting material for synthesis of new adsorbents, composites, and catalysts. In addition, a synthesis of carbon nanofibers and nanotubes has become a new research area in material science. For the synthesis of carbon nanotubes several methods have been developed, mainly carbon-arc production or plasma decomposition of hydrocarbons but these tubules always form together with a significant amount of other carbon products such as fibre and soot. The advent of electron microscopy made it possible to discover and describe a number of morphological types of carbon filaments formed on the catalysts. Various types of carbon may be formed. It was distinguished up to seven different types of carbon. Since natural gas which methane is the main component is the cheapest hydrocarbon feedstock, it is another feature of large scale production of carbon nanofibers and nanotubes.  Decomposition of methane is a well-known process. It was practiced batch-wise using firebrick contact and required elevated temperatures for the production of carbon black with hydrogen being used as a supplemental gaseous fuel. Attempts have been made to use catalysts to reduce the maximum temperature of the decomposition of methane and at the same time to control the morphology of the carbon nanotubes forming. The main focus of this paper is to report a new method for producing carbon nanotubes. In this method, carbon nanotubes are catalyzed by a novel catalyst based on Ni/Mn using methane as feedstock. We demonstrate for the first time, that Ni/Mn catalyzes single wall carbon nanotubes and that methane can be used as feedstock for single wall carbon nanotubes. Transmission Electron Microscope images showing a catalytic particle attached to the end of single wall carbon nanotubes reveal a clear correspondence between particle and the carbon nanotube. That this simple correspondence has never before been observed with Ni/Mn catalyst or in the arc or by laser-vaporization strongly suggests distinct mechanisms existing for single wall carbon nanotube production. Here we would like to explicate the morphology of carbon formed on Ni/Mn-based catalyst used for the decomposition of methane.